## Slide 1: Controlling Traveling-Wave Phonons at Room Temperature
Joel N. Johnson
April 25th, 2025
Northern Arizona University

## Slide 2: Brillouin Scattering: Optomechanical Coupling

## Slide 3: Brillouin Scattering: Optomechanical Coupling
Phase (velocity) matching:

## Slide 4: Brillouin Scattering: Optomechanical Coupling
Phase (velocity) matching:
Energy Conservation:
Momentum Conservation:
✓
✓

## Slide 5: Brillouin Scattering: Optomechanical Coupling
Phase (velocity) matching:
Energy Conservation:
Momentum Conservation:
✓
✓

## Slide 6: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light

## Slide 7: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals

## Slide 8: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals
Brillouin-Induced Raman Modes
  Harnessing sound for engineered behaviors

## Slide 9: Laser Cooling
Why do we care about laser cooling?
  Reduce thermal noise
  Access quantum regimes

## Slide 10: Laser Cooling
Why do we care about laser cooling?
  Reduce thermal noise
  Access quantum regimes
Demonstrated for discrete cavity systems
  Resonant cavities permit discrete modes
  Tune laser just red of cavity resonance  discrete mode cooling

## Slide 11: Laser Cooling of a Continuum of Modes
Fast escape condition
  Remove phonons faster than they are replenished:

## Slide 12: Laser Cooling of a Continuum of Modes
Fast escape condition
  Remove phonons faster than they are replenished:
Challenging because scattered power scales with length:

## Slide 13: Laser Cooling of a Continuum of Modes
Fast escape condition
  Remove phonons faster than they are replenished:
Challenging because scattered power scales with length:
Gain
Power
Thermal

## Slide 14: Laser Cooling of a Continuum of Modes
Otterstrom et al. 2018: Chip waveguide
  Extremely high engineered gain:

## Slide 15: Laser Cooling of a Continuum of Modes
Otterstrom et al. 2018: Chip waveguide
  Extremely high engineered gain:
Challenging in fiber
  Typical fiber has very low gain:
  Requires large enough gain for small enough length for fast escape

## Slide 16: Solution: CS2
Carbon disulfide (CS2) is a very high gain liquid

## Slide 17: Solution: CS2-Filled Liquid-Core Optical Fiber
Carbon disulfide (CS2) is a very high gain liquid
Fill hollow-core optical fiber with CS2:
SMF-28
UHNA7
hollow-core
UHNA7
SMF-28
~1.68 µm
1 meter

## Slide 18: Solution: CS2-Filled Liquid-Core Optical Fiber
Carbon disulfide (CS2) is a very high gain liquid
Fill hollow-core optical fiber with CS2:
SMF-28
UHNA7
hollow-core
UHNA7
SMF-28
~1.68 µm
1 meter

## Slide 19: Solution: CS2-Filled Liquid-Core Optical Fiber
Carbon disulfide (CS2) is a very high gain liquid
Fill hollow-core optical fiber with CS2:
SMF-28
UHNA7
hollow-core
UHNA7
SMF-28
~1.68 µm
1 meter

## Slide 20: Liquid-core Optical Fiber Sample

## Slide 21: Liquid-core Optical Fiber Sample

## Slide 22: Liquid-core Optical Fiber Sample
CS2 enters here

## Slide 23: Liquid-core Optical Fiber Sample
CS2 enters here

## Slide 24: Cooling Figure of Merit
All materials have a natural rate of mechanical dissipation (Γ0)

## Slide 25: Cooling Figure of Merit
All materials have a natural rate of mechanical dissipation (Γ0)
To cool is to increase dissipation rate (Γ+)

## Slide 26: Cooling Figure of Merit
All materials have a natural rate of mechanical dissipation (Γ0)
To cool is to increase dissipation rate (Γ+)
Spectral linewidth gives dissipation rate
Γ

## Slide 27: Cooling Figure of Merit
All materials have a natural rate of mechanical dissipation (Γ0)
To cool is to increase dissipation rate (Γ+)
Spectral linewidth gives dissipation rate
Broadened linewidth gives measure of cooling
Γ

## Slide 28: Cooling Figure of Merit
Broadened linewidth gives measure of cooling

## Slide 29: Cooling Figure of Merit
Broadened linewidth gives measure of cooling:

## Slide 30: Cooling Figure of Merit
Broadened linewidth gives measure of cooling:

## Slide 31: Cooling Figure of Merit
Broadened linewidth gives measure of cooling:

## Slide 32: Cooling Figure of Merit
Broadened linewidth gives measure of cooling:

## Slide 33: Cooling Figure of Merit
Broadened linewidth gives measure of cooling:
C-Value (% cooled)

## Slide 34: Experimental Setup

## Slide 35: Results
Γ

## Slide 36: Results
Γ

## Slide 37: Results
cooling from room temperature
Γ

## Slide 38: Results
C-Value
Γ

## Slide 39: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals

## Slide 40: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals

## Slide 41: Brillouin Spectroscopy
What is Brillouin spectroscopy?
  Measurement of mechanical properties of materials
  Obtain mechanical resonances, elastic moduli

## Slide 42: Brillouin Spectroscopy
What is Brillouin spectroscopy?
  Measurement of mechanical properties of materials
  Obtain mechanical resonances, elastic moduli
Where is it used?
  Biomechanics and medical diagnostics
  Distributed fiber-optic strain and temperature monitoring along structures

## Slide 43: Traditional Brillouin Scattering
Spontaneous Brillouin scattering
  Thermal phonons

## Slide 44: Traditional Brillouin Scattering
Spontaneous Brillouin scattering
  Thermal phonons
Stimulated Brillouin scattering
  Inject Stokes seed
  Self-reinforcing process

## Slide 45: Traditional Brillouin Scattering
Would be nice to drive with Stokes
  Problem: drowns the signal

## Slide 46: Coherently Stimulated Brillouin Scattering?
Would be nice to drive with Stokes
  Problem: drowns the signal
Separate, shifted probe laser?
  Incoherent with driven phonon mode
  Would not “talk” to the driven phonons (unphase-matched)

## Slide 47: Phase Matching Relaxation
At small scales, position certainty means momentum uncertainty
Heisenberg uncertainty principle

## Slide 48: Phase Matching Relaxation
At small scales, position certainty means momentum uncertainty
Wavevector describes momentum of a wave

## Slide 49: Phase Matching Relaxation
At small scales, position certainty means momentum uncertainty
Wavevector describes momentum of a wave
Pump-probe detuning

## Slide 50: Cheating Phase Matching
1 meter sample
  picometers preserves 50% of signal

## Slide 51: Cheating Phase Matching
1 meter sample
  picometers preserves 50% of signal
1 centimeter sample
  picometers preserves 83% of signal!
  36 picometers is 4.5 GHz, enough for a filter to separate!

## Slide 52: Coherently Stimulated Brillouin Spectroscopy
Allows Stokes driving while preserving coherence with a shifted probe

## Slide 53: Coherently Stimulated Brillouin Spectroscopy
Allows Stokes driving while preserving coherence with a shifted probe
~1 million times more powerful than traditional SBS!

## Slide 54: CoBS vs StimBS vs SponBS
Spontaneous BS
Stimulated BS
CoBS

## Slide 55: CoBS vs StimBS vs SponBS

## Slide 56: CoBS:

## Slide 57: CoBS:

## Slide 58: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals
Brillouin-Induced Raman Modes
  Harnessing sound for engineered behaviors

## Slide 59: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals
Brillouin-Induced Raman Modes
  Harnessing sound for engineered behaviors

## Slide 60: Explore Brillouin/Raman Transition
Brillouin
Travelling-wave phonons in bulk material
Travelling Wave Phonons
CoBS

## Slide 61: Explore Brillouin/Raman Transition
Brillouin
Travelling-wave phonons in bulk material
Travelling Wave Phonons
Standing Wave Phonons
Raman
Standing wave phonons in molecular vibrations
CoBS

## Slide 62: Explore Brillouin/Raman Transition
Brillouin
Travelling-wave phonons in bulk material
Travelling Wave Phonons
Standing Wave Phonons
Raman
Standing wave phonons in molecular vibrations
Start in Brillouin domain and approach Raman-like modes
CoBS

## Slide 63: Reflected Phonons Create Standing Waves
Ω
Ω

## Slide 64: In-Phase Phonons Constructively Interfere
Ω
Ω

## Slide 65: In-Phase Phonons Constructively Interfere
Ω
Ω

## Slide 66: In-Phase Phonons Constructively Interfere
Ω
Ω

## Slide 67: In-Phase Phonons Constructively Interfere
Ω
Ω

## Slide 68: Gain of Relevant Materials

## Slide 69: 1 cm Germanium-Doped Fiber

## Slide 70: 1 mm Germanium-Doped Fiber

## Slide 71: 1 cm CS2

## Slide 72: 4 mm CS2

## Slide 73: 1 μm TeO2

## Slide 74: 1 μm TeO2 Again
5 MHz bins
10 MHz bins

## Slide 75: 1 mm CS2

## Slide 76: 100 μm CS2

## Slide 77: Suspended Silica Chip Waveguide

## Slide 78: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light

## Slide 79: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals

## Slide 80: Controlling Sound with Light
Laser Cooling of Traveling-Wave Phonons in an Optical Fiber
  Quieting sound with light
Coherently stimulated Brillouin Scattering (CoBS)
  Amplifying sound to measure subtle signals
Brillouin-Induced Raman Modes
  Harnessing sound for engineered behaviors

## Slide 81: Acknowledgements

## Slide 82: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
phonon
Ω

## Slide 83: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
Laser light
phonon
Ω
⍵P

## Slide 84: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off approaching sound wave (Brillouin scattering)
phonon
Ω
⍵P

## Slide 85: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off approaching sound wave (Brillouin scattering)
Energy transfers from sound to light:
  Returning light is frequency upshifted (blue-shifted)
phonon
Ω
⍵P
⍵aS = ⍵P + Ω

## Slide 86: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off approaching sound wave (Brillouin scattering)
Energy transfers from sound to light:
  Returning light is frequency upshifted (blue-shifted)
  Sound wave intensity is lowered (cooled)
phonon
Ω
⍵P
⍵aS = ⍵P + Ω

## Slide 87: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off approaching sound wave (Brillouin scattering)
Energy transfers from sound to light:
  Returning light is frequency upshifted (blue-shifted)
  Sound wave intensity is lowered (cooled)
phonon
Ω
⍵P
⍵aS = ⍵P + Ω

## Slide 88: Optomechanical Cooling
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off approaching sound wave (Brillouin scattering)
Energy transfers from sound to light:
  Returning light is frequency upshifted (blue-shifted)
  Sound wave intensity is lowered (cooled)
phonon
Ω
⍵P
⍵aS = ⍵P + Ω
anti-Stokes

## Slide 89: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
phonon
Ω

## Slide 90: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
Laser light
phonon
Ω
⍵

## Slide 91: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off retreating sound wave (Brillouin scattering)
phonon
Ω
⍵

## Slide 92: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off retreating sound wave (Brillouin scattering)
Energy transfers from light to sound:
  Returning light is frequency downshifted (red-shifted)
phonon
Ω
⍵
⍵’ = ⍵ - Ω

## Slide 93: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off retreating sound wave (Brillouin scattering)
Energy transfers from light to sound:
  Returning light is frequency downshifted (red-shifted)
  Sound wave intensity is increased (heated)
phonon
Ω
⍵
⍵’ = ⍵ - Ω

## Slide 94: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off retreating sound wave (Brillouin scattering)
Energy transfers from light to sound:
  Returning light is frequency downshifted (red-shifted)
  Sound wave intensity is increased (heated)
phonon
Ω
⍵
⍵’ = ⍵ - Ω

## Slide 95: Optomechanical Heating
Material at room temperature has thermal fluctuations (phonons)
Laser light backscatters off retreating sound wave (Brillouin scattering)
Energy transfers from light to sound:
  Returning light is frequency downshifted (red-shifted)
  Sound wave intensity is increased (heated)
phonon
Ω
⍵
⍵’ = ⍵ - Ω
Stokes

## Slide 96: Optomechanical Heating

## Slide 97: Amplitudes: Experiment A

## Slide 98: Amplitudes: Experiment A

## Slide 99: Amplitudes: Experiment A

## Slide 100: LCOF Fabrication

## Slide 101: Cooling Experiment B

## Slide 102: Cooling Experiment B

## Slide 103: Cooling Experiment B

## Slide 104: Cooling Experiment B

## Slide 105: Cooling Experiment B

## Slide 106: Phase Matching Bandwidth
5 GHz
14.5 GHz
Pump-probe separation
26.5 GHz
37 GHz

## Slide 107: Sub-10 fW Sensitivity

## Slide 108: P, S, Pr Contribute Equally

## Slide 109: Fano Resonance
Interference between the signal and the broad background continuum
Occurs when signal intensity is on the order of the background
Relative phases determine asymmetry

## Slide 110: Fano Resonance
Naïve Lorentzian Fit
Fano Fit

## Slide 111: Elastically-Suspended Photonic-Phononic